## Slide 1: Recyclability drives adhesive development
Fred Gustafson, Ph. D
Adherent Laboratories, Inc.
St. Paul, Minnesota
fred.gustafson@adherentlabs.com
www.adherentlabs.com

## Slide 2: Contents
Recycling rates in the US
Paper recycling
  Impact of adhesives
  Test methods
  PSA products: labels, tape, and notes
PET bottle and thermoform recycling
  Impact of adhesives
  Test methods
  PSA labels
Business considerations
Solving the problem

## Slide 3: Recycling rates in the US
65.1%
AF&PA
47.8 MM lb
NAPCOR
Rate not available
31%
APR
91%
CPA
67%
Al Assoc.
38%
EPA
95%
Autobytel
27.8%
CRI

## Slide 4: Citations – recycling rates
Al Assoc. – Aluminum Association
Autobytel – Automobile web site
AF&PA – American Forest and Paper Association
APR – Association of Postconsumer Plastic Recyclers
CPA – Corrugated Packaging Alliance
CRI – Container Recycling Institute
EPA – US Environmental Protection Agency
NAPCOR – National Association for PET Container Resources

## Slide 5: Adhesive products impacting recycling
Sticky Stamps
Tape
Repositionable Notes
Paper Labels
Labels for PET food containers
Labels for PET bottles

## Slide 6: Paper recycling facts
Recycling rate for paper is 65% and for corrugated is 91% (2012)
70 MM tons of paper and corrugated are recycled in the US every year
Adhesives are contaminants and must be removed from paper during recycling
  Adhesives are more of a problem with fine paper than corrugated
Adhesive contamination is a huge cost to the recycled paper industry
  Recycling mill down time and clean up cost
  Estimated cost was over $500 MM per year in the 1990’s
Recycled paper companies still complaining about adhesives

## Slide 7: Contaminants in recycled paper
Must be removed during the recycling process
Plastic – CD’s and folders
Metals – staples and paper clips
Ink and toner powder
Color – dyes and pigments
Coatings – coated paper
Adhesives

## Slide 8: Adhesives and paper recycling
Water insoluble adhesives
  Adhesives will adhere to the wire of a paper machine
  Causes a repeating hole in the paper
  Expensive clean up required
Water soluble adhesives
  Adhesives build up in the waste water of the recycling mill
  Adhesives can precipitate with a pH or temperature change
  Expensive clean up required

## Slide 9: Paper recycling unit operations
Pulping
  Water and agitation turns paper into pulp
Screening with slotted screen
  Removes large contaminants > 100 um diameter
Flotation – air bubbles and surfactant
  Foam carries small particles to the surface with the foam
Centrifugal cleaning - spinning
  Removes light or heavy contaminants
Dispersion and washing
  Removes small contaminants, inks and fillers by filtration
Bleaching with hydrogen peroxide
  Removes color
Recycled paper pulp

## Slide 10: Pulping, screening, and flotation
Pulper
Screen
Flotation

## Slide 11: Adhesive removal
Waste paper is pulped in a large tank (pulper)
  Avoid shredding of adhesive into smaller particles
Large adhesive particles are removed by a series of slotted screens
  Smallest screen is typically 0.004” or 100 µm opening
Small adhesive particles are removed by flotation
  Surfactant and air will bring small contaminants to the surface as a foam
  Optimal size for removal is about 20 – 100 µm

## Slide 12: Acrylic pressure sensitive adhesives
Many acrylic adhesives will extrude through the screens
Particles are then too large to be removed by flotation
Solution
  Increase the elastic modulus of the adhesive so that will be removed by screens rather than extrude through the screen
  Facestock and adhesive surface properties also impact removal efficiency
Reference:
  Controlling Adhesive Behavior during Recycling, Carl Houtman, et. al, 7th Research Forum on Recycling, Pulp and Paper Technical Association of Canada, 2004

## Slide 13: Test protocols for labels (Adhesives on paper products)
Tag and Label Manufacturers Institute (TLMI) web site:
  tlmi.com/sustainability
Introduction to Recycling Compatible Adhesives
Specification for Paper Labels Coated with Recycling Compatible Pressure Sensitive Adhesives
Laboratory Testing Protocol for Paper Labels Coted with Recycling Compatible Pressure Sensitive Adhesives
Mill Recycling Trial Protocol
Image Analysis Protocol - Determination of Adhesives in Paper Handsheets by Image Analysis

## Slide 14: Self Adhesive Stamps
Introduced by the USPS in 1991
  Popular with consumers, but protested by the recycled paper industry
USPS funded project on “Environmentally Benign Adhesives”
  Adhesive suppliers, converters, and paper industry participation
  Developed test methods for adhesive removal from paper
  Developed adhesives that were removed at 99.9% in laboratory test
  Tested the stamps in six recycling mills in the US
  Developed a specification for stamps with benign adhesive
Key improvement > 90% of adhesive removable by screens
Converted all sticky stamps to benign adhesives in the year 2000
Reference:
  USPS-P-1238F, Specification, Pressure Sensitive Adhesive Stamp

## Slide 15: PSA Paper Labels
Recycling compatible stamp adhesives also work for paper labels
TLMI (Tag and Label Manufacturers Institute) Committee on Recycling Compatible Adhesives (RCA)
  Issued the specifications and test methods previously cited
  Worked with adhesive suppliers to encourage development of better adhesives
  Worked with converters to promote recycling compatible adhesives
Recycling compatible paper labels are available for retail and commercial applications
  Estimated adoption rate is less than 50%
Fred Gustafson
Street Address
Bloomington, MN 55438

## Slide 16: Repositionable notes and labels
Microsphere adhesives
  Common adhesive technology but not the only technology
  Microsphere adhesives are too small to be removed by screens
  Flotation is the best method to remove the adhesive
Solution
  Test products for adhesive removal by TLMI test protocols
  Optimize adhesive size and chemistry for removal by flotation
  Stripe coating reduces overall adhesive coating weight

## Slide 17: 3M experience with repositionable products
Most paper recyclers banned repositionable notes in the 1990’s
  Some businesses and government offices stopped buying the product
Testing
  Laboratory and mill scale experiments
  USPS and TLMI protocols for recycling compatible adhesives
Adhesive optimization R & D
  Discovered control handles on adhesive removal
  Commercialized better adhesives
Product claim: All Post-it® Notes and Easel Pads are recyclable
  Product contains recycling compatible adhesive. During the paper recycling process, the paper is recycled and the adhesive is removed.

## Slide 18: Film Tapes and Labels
Adhesive is coated on a polymeric backing
Pulping and screening
  The plastic backing remains intact during pulping
  Removed by screens
Potential problem
  If the adhesive is separated from the backing during pulping, the adhesive can contaminate the pulp
Solution
  Reformulate the adhesive
  Develop a primer that keeps the adhesive attached to the backing in water

## Slide 19: PET bottle and thermoform recycling
Adhesives come from the labels on PET bottle or thermoform
Labels must be removed from the PET material during recycling
Contamination caused by adhesive, paper, or ink:
Residuals – organic material will char when the recycled flake is extruded to make a new product
Residuals can contaminate the recycling equipment
Black specs from ink will carry over into new product
Fluorescence from residual components is unwanted

## Slide 20: Test Protocol for PET Thermoforms
Sample preparation
  Mix PET flake with water, 0.3% surfactant, and 1% NaOH
  Heat to 88°C for 15 minutes with agitation
  Remove floatables and sinking solids
  Rinse with water
Testing
  Color of dry flake
  Fluorescence of dry flake
  Black specs over 10 mils (0.1”) diameter
  Reference: Association of Postconsumer Plastic Recyclers
  Protocol for Evaluating PET Thermoform Labels and Adhesives for Compatibility with PET Recycling

## Slide 21: Key learning
Contamination of flake is caused by adhesives, backing, and inks
Best label properties
  Label completely removed from the PET surface under the test conditions
  Filmic backings appear to leave fewer contaminants than paper backings
More work needs to be done to identify the best label properties
Active collaboration between:
  Adhesive suppliers
  TLMI – Tag and Label Manufacturers Institute
  APR – Association of Postconsumer Plastic Recyclers
  NAPCOR – National Association for PET Container Resources

## Slide 22: Traditional adhesive life cycle
End User
Disposal
Landfill
Adhesive
Product
Old Paradigm

## Slide 23: New paradigm
End User
Recycler
New Product
Adhesive
Product
Feedback
Adhesive removal

## Slide 24: Advantages of compliance
Triple bottom line
  Profit, stakeholders, and environment
Make product claims with the test protocols
  My product does not interfere with recycling
Avoid loss of business
Participate in joint development projects
  Share the costs of technology development
  Keep up with inevitable technology advancement
Counterbalance: cost of research and development

## Slide 25: Model for recyclability research projects
Lead organization to organize or sponsor research
Participation by adhesive, product, and recycling industries
Research program with shared results
Confidentiality of adhesive compositions
  Adhesives identified by type only
Equitable distribution of cost
Test method development
Specification
Adoption by the industry

## Slide 26: Adherent Laboratories, Inc. St. Paul, Minnesota
Adhesive, sealant, and coating specialist company
Laboratory services
  Adhesive and raw material development
  Laboratory coating and adhesive evaluation
  Core competency in hot melt adhesives
Consulting services
  Adhesive specifications
  Market and technology assessment
  Product design and failure analysis
Web site: www. adherentlabs.com
Changing the way you look at adhesives